Supporting Information

Reversible switching of electromagnetically induced transparency in phase change metasurfaces

Libang Mao1, Yang Li1,2, Guixin Li2, Shuang Zhang3, and Tun Cao1,*

1School of Optoelectronic Engineering and Instrumentation Science, Dalian University of Technology, Dalian 116024, China

2Department of Materials Science and Engineering, Southern University of Science and Technology, Shenzhen 518055, China

3School of Physics & Astronomy, University of Birmingham, Birmingham B15 2TT, UK

Figure S1. The fabrication scheme of the EIT phase-change metasurface.

Table S1. The fitting parameters for the transmittance spectra of the phase change metasurfaces using the coupled harmonic Lorentz oscillator model

|  | ω0 | δ | γ1 | γ2 | κ | g |
| --- | --- | --- | --- | --- | --- | --- |
| AD-AM | 156 THz | 18 THz | 25 THz | 12 THz | 27 THz | -14 THz |
| CR | 137 THz | 18 THz | 22 THz | 51 THz | 1 THz | -9 THz |